Abstract

Biodegradable starch-glycerol based films were obtained. The influence of lipid compounds (palmitic, stearic and oleic acid), other polymers (hydroxypropylmethylcellulose and sodium caseinate) and bioactive compounds (α-tocoferol, D-limonene and orange essential oil) on film properties (oxygen and water vapour barrier, optical, mechanical, nano- and microstructural). Furthermore the effect of storage time on films’ properties was also considered.

Fatty acids addition did not improve the water vapour ability of films except for non-stored saturated fatty acids containing films. X-ray diffraction results showed that cristallinity of films increased with storage time, thus increasing the stiffness and decreasing the gloss of films. Furthermore, crystallinity affected the water sorption capacity of films as function of relative humidity and temperature. Glass transition temperature of starch films varied with saturated fatty acids addition. However, oleic acid did not affect this parameter. The presence of fatty acids promoted the formation of V-type structures, thus indicatin the formation of amylose-lipid complexes that inhibited the developmet of other crystalline structures.

The effect of the incorporation of other biopolymers to improve the functionality of starch films was also studied. Hydroxypropylmethylcellulose (HPMC) addition inhibited starch retrogradation. However, obtained films were more permeable, specially in case of oxygen. HPMC addition produced phase separation as it was observed by scanning electron microscopy. On the contrary, sodium caseinate incorporation (NaCas) allowed to obtain homogeneous films and less permeable to oxygen. Obtained films showed less mechanical resistance in comparison with pure starch films but a greater flexibility without increasing the water vapour permeability. Rearrangement of polymers chains during storage reduced the mechanical resistance, the extensibility and the gloss of composite films. Regarding the obtained results, the film including a starch:protein ratio of 50:50 was choosen as the film with the most adequate properties.

Composite film (starch:Nacas ratio = 50:50) was studied as a matrix for the incorporation o active compounds (α-tocopherol, D-limonene and orange essential oil). The effect of α-tocopherol addition was compared with the incorporation of oleic acid and their mixture. Lipids addition promoted phase separation between starch and NaCas due to the different interactions between each polymer and the lipids. Furthermore, oleic acid addition increased significantly the oxygen permeability whereas α-tocopherol greatly improved the antioxidant capacity of films without affecting the oxygen permeability.

D-limonene and orange essential oil incorporation was carried out by forming rapeseed and soy nanoliposomes, which acted as carriers of bioactive components. Nanoliposomes incorporation was performed directly in starch-NaCas dispersions without any homogenization, to avoid nanoliposomes damages. Bioactive compounds addition did not confer antimicrobial capacity to the films (except for soy-orange oil nanoliposomes containing film) probably due to the high stability of nanoliposomes and the low antibacterial activity of D-limonene and orange essential oil.